## Slide 1: DFT-analysis of 3D & 2D model of MoS2 [2H] Density of states & band structure
Notes: Ikke snakk så altfor mye her.

## Slide 2: Crystal structure
MoS2 [2H], classified as transition metal dichalcogenide (TMD)
Hexagonal crystal structure as indicated by [H]
Initial lattice paramteres given by POSCAR-file: a = 3.190Å and c = 14.879Å
Bulk and monolayer MoS2 2H, consist of 6 and 3 atoms respectively.
Trigonal prismatic arrangment of MoS2 [2H]
Notes: -2 indicates that the unitcell containes 2 layers.
-purple ball is Molybednum, yellow sulphide
-Trigonal prismatic arrangment means that the sulphides atoms is symmetric around the Molybednum atom.

## Slide 3: Creation of monolayer MoS2 [2H]
Gradually increasing the vacuum layer with 2Å
tag IVDW = 1 inserted in INCAR-file
12Å where used as converged vacuum layer.
Tab.1 Vacuum layer inserted in c-direction in the initial POSCAR-file.
Notes: Van der Waals forces acting between the layers. Inserting IVDW = 1, illustrating Van der Waals forces.

## Slide 4: Convergence of energy cut-off
Relative total energies: Erel = Etot[bulk] – Etot [slab]
Energy cut-off step-size of = 50 eV
Convergence of Erel was found to be 450eV

## Slide 5: Convergence of k-points density
Relative total energies: Erel = Etot[bulk] – Etot [slab]
k-points denisity step-size 1
Convergence of Erel was found to be at k-points density set to 5.
Gamma centered mesh with grid points for bulk and for slab structure.
Notes: -Hexagonal structure, preferred to use gamma centered mesh.
-reason for 10x10x1 is due to increased vacuum layer increases the lattice parameter c, giving a "small" dimension in reciprocal space. Do not need many k-points in c-direction then.

## Slide 6: Relaxtion of bulk MoS2
Poor initial guess of atomic position.
INCAR-tag IBRION = 2
Initial lattice parameters set to: a = 3.190Å and c = 14.879Å, which yields a c/a-ratio of 4.66
After relaxation the new lattice parameters where calculated to a = 3.188Å and c = 12.403Å, with a c/a-ratio of 3.89
c/a-ratio has decreased with approximately 16.5%
In good agreement with experimental values of c/a = 3.90 [1]
Notes: IBRION = 1 Close to the local minimum
IBRION = 2 conjugate gradient algorithm

## Slide 7: Density of states
VASP using PAW-PBE potential with PE-GGA functional.
Notes: -Point to bandgap, larger for monolayer than bulk.
-Higher density of states near valence band for monolayer compared to bulk.
- Peaks in DOS is Hove singularites, where the slope of DOS changes discontinously

## Slide 8: Band structure
Bulk MoS2 [2H] exhibits an indirect bandgap
Monolayer MoS2 [2H] exhibits a direct bandgap
high-symmetry path: Γ − M − K − Γ
Notes: Bulk - gamma centered bandgap.
Monolayer - K-centered bandgap

## Slide 9: Band structure
Tab.2 Bandgap of both structures shown for DFT-calculations using PE-GGA functional and experimental values [2] [3]

## Slide 10: Band structure
Tab.2 Bandgap of both structures shown for DFT-calculations using PE-GGA functional and experimental values [2] [3]
Grossly underestimates experimental bandgap
Relative error for bulk:
Relative error for monolayer:

## Slide 11: Applications of monolayer & DFT-Improvements
Beneficial in application such as:
  Photodetectors
  Photovoltaics
  Photocatalysis

## Slide 12: Applications of monolayer & DFT-Improvements
Beneficial in application such as:
  Photodetectors
  Photovoltaics
  Photocatalysis
Improvments of DFT-calculation:
  Hybrid functional; HSE06 functional

## Slide 13: References
[1] Wakabayashi, N., Smith, H. G., & Nicklow, R. M. (1975). Lattice dynamics of hexagonal Mo S 2 studied by neutron scattering. Physical Review B, 12(2), 659.
[2] Lee, C., Yan, H., Brus, L. E., Heinz, T. F., Hone, J., & Ryu, S. (2010). Anomalous lattice vibrations of single-and few-layer MoS2. ACS nano, 4(5), 2695-2700.
[3] Mak, K. F., Lee, C., Hone, J., Shan, J., & Heinz, T. F. (2010). Atomically thin MoS 2: a new direct-gap semiconductor. Physical review letters, 105(13), 136805.